Comprehensive Mechanical Integrity & Fitness-For-Service Assessment Report

Crude Distillation Unit (CDU-1) — Heat Exchanger E-204

Author: SOVA Industrial Reliability & Mechanical Integrity Division   |   Date: 27 September 2026   |   Classification: Confidential • Strictly Air-Gapped

EXECUTIVE SUMMARY A formal 4-part fitness-for-service evaluation of Heat Exchanger E-204 per API 579-1. Evaluates ultrasonic thickness readings, corrosion rates, remaining safe operating life, and scheduled maintenance requirements.

1. Executive Summary & Facility Context

This comprehensive technical assessment report establishes the mechanical integrity and remaining safe operating lifespan for Heat Exchanger E-204 located within Crude Distillation Unit CDU-1.

All calculations adhere strictly to API 579-1 / ASME FFS-1 Fitness-For-Service standards, ASME Section VIII Division 1 Boiler and Pressure Vessel Code, and plant reliability mandates.

Assessment Standard: API 579-1 Part 4 (General Metal Loss) Level 1 Assessment

Operating Pressure: 18.2 bar design / 14.5 bar normal operating threshold

Operating Temperature: 185 deg C inlet / 130 deg C outlet

2. Ultrasonic Thickness Measurement (UTM) Empirical Data

Ultrasonic thickness inspection was completed on 18 September 2026 across 24 critical Thickness Measurement Locations (TMLs). The nominal specification is SA-516 Gr. 70 carbon steel with nominal wall thickness of 10.0 mm.

Table: Summary of Critical TML Inspection Points

| TML Tag | Location / Component | Nominal (mm) | Measured (mm) | Loss (mm) | Corrosion Rate (mm/yr) |
| --- | --- | --- | --- | --- | --- |
| TML-01 | Shell Course 1 Top | 10.0 | 9.6 | 0.4 | 0.08 |
| TML-07 | Shell Course 2 Bottom | 10.0 | 9.1 | 0.9 | 0.12 |
| TML-14 | Channel Side Inlet | 10.0 | 8.2 | 1.8 | 0.15 |
| TML-19 | Channel Side Return Nozzle | 10.0 | 8.4 | 1.6 | 0.14 |
| TML-24 | Floating Head Cover | 12.0 | 11.2 | 0.8 | 0.09 |

3. Mathematical Modeling & Code Computations

The minimum required retirement wall thickness (t_min) is determined per ASME Section VIII Division 1 UG-27 equation for cylindrical shells under internal design pressure:

1. Step 1: Compute circumferential hoop stress and minimum thickness requirement (7.0 mm).

2. Step 2: Establish remaining corrosion allowance across governing location TML-14 (1.2 mm).

3. Step 3: Compute remaining operating lifespan based on maximum observed corrosion rate (8.0 years).

# API 579-1 Level 1 Calculation for Cylindrical Shell P = 18.2 # Design Pressure (bar) R = 600.0 # Inside Radius (mm) S = 138.0 # Allowable Stress for SA-516 Gr.70 (MPa) E = 1.0 # Joint Efficiency (Full Radiography) # t_min = (P * R) / (S * E - 0.6 * P) t_min = (1.82 * 600.0) / (138.0 * 1.0 - 0.6 * 1.82) # Result: t_min = 7.02 mm (Design Retirement Limit: 7.0 mm) remaining_ca = 8.2 - 7.0 # Remaining Corrosion Allowance = 1.2 mm remaining_life = remaining_ca / 0.15 # Remaining Life = 8.0 Years

4. Engineering Recommendations & Action Plan

Heat Exchanger E-204 is approved for continued safe operation under current design conditions. However, the localized thinning at TML-14 requires increased inspection frequency.

An ultrasonic reinspection is scheduled for Q3 2027 to verify that corrosion rates do not accelerate.

Next Inspection Date: September 2027 (12-month interval)

Action Item: Install online ultrasonic corrosion monitoring sensors at TML-14 and TML-19

Corrosion Inhibitor: Maintain neutralizer dosing at CDU overhead accumulator to minimize acid condensation